☎ : 905-487-3428   🌐 : www.acmetex.com  Warehouse Location: Toronto · Edmonton

ACME-KSS3/3 Para-Aramid with 316 stainless steel wire sewing thread

Description: KSS3/3 Para-Aramid(Kevlar by Dupont) is made with 100% Polytetrafluoroethylene (PTFE), making it extremely lubricant and durable which allows it to for better hook pickup, lower elongation and strength for few knots and breaks. It also provides a 316 stainless steel sewing thread offer the strong tensile strength while the 316 with high Inconel stainless steel wire provides excellent chemical resistance. Advantages: - Heat resistant - Chemical resistant - Good sewability - Flexibility - Good tensile strength; Applications: - Welding blanket/curtains - Expansion joints - High temperature insulation - Heat shield/containment - Gaskets & over-door seals - Removable insulation cover - Filter bag.

Property Data KSS3/3

Material; Para-Aramid with 316 stainless steel wire. Twist; 3 ply with 3 wire. Tensile strength(lbs); Approx. 27. Final Twist; “Z”. Para-Aramid Decomposition Point; Approx. 878°F (470°C). Stainless Steel Melting Point; Approx. 2552°F (1400°C). Size of the thread; 0.011”. Weight per spool; About 1.1 lbs(500 grams).